
Specification

Extrusion: SQUARE 21



1. The extrusion shall be made of aluminum alloy EN AW 6060 T66.
2. The extrusion shall be available in following surface finishes:
   * Blank
   * Anodized natural (thickness 15µm)
   * Anodized black (thickness 15µm)
   * Coated with polyester powder-coating in all standard RAL-colors
3. The extrusion shall have following dimensions: 20,7mm x 25mm.
4. This extrusion shall fit a PCB of maximum 15mm.
5. The extrusion shall be available in lengths up to 6m.
6. The extrusion shall be compatible with an aluminum click profile of following dimensions: 20mm x3,3mm.
7. The extrusion shall have a compatible fully closed endcap.
8. The extrusion shall have compatible endcap with hole for cable.
9. The extrusion shall have a compatible flat PMMA cover.