
Specification

Extrusion: RECTANG 24



1. The extrusion shall be made of aluminum.
2. The extrusion shall be available in following surface finishes:
   * Blank
   * Anodized natural (thickness 15µm)
   * Anodized black (thickness 15µm)
   * Coated with polyester powder-coating in all standard RAL-colors
3. The extrusion shall have following dimensions: 24mm x 18,25mm.
4. The extrusion shall fit a PCB with a width of maximum 8mm.
5. The extrusion shall be available in lengths up to 6m.
6. The extrusion shall be compatible with following extruded PMMA covers:
   * Flat cover 5mm
   * Square cover 16,25mm
   * Round cover 16,25mm
   * Lens cover 11,7mm
7. These covers shall be available in maximum 3m length.
8. The extrusion shall be compatible with a clicking profile with following dimensions: 24mm x 8,7mm
9. The extrusion shall have a compatible fully closed endcap.
10. The extrusion shall have a compatible endcap with a hole for a cable.