
Specification

Extrusion: SQUARE 45



1. The extrusion shall be made of aluminum alloy EN AW 6060 T66.
2. The extrusion shall be available in following surface finishes:
   * Blank
   * Anodized natural (thickness 15µm)
   * Anodized black (thickness 15µm)
   * Coated with polyester powder-coating in all standard RAL-colors
3. The extrusion shall have following dimensions: 45mm x 42mm.
4. The extrusion shall be available in lengths up to 6m.
5. The extrusion shall be compatible with an extruded PMMA cover.
6. The extrusion shall have a compatible fully closed endcap.